SkyBase® Premium Basecoat color is designed to provide excellent coverage, fast dry times, and great metallic control.  This polyester and acrylic blended basecoat features easy repairability with no wrinkling.

| Product Cross Reference Information Product comparisons are based on a similar product replacement. Performance and mix ratios may vary. |
| --- |
| DuPont | PPG | SW | BASF |
| ChromaBase® | Deltron® DBC | Ultra 7000 Basecoat® | Limco 1-2-3® |

### DIRECTIONS FOR USE

Application recommendations are for an ambient shop temperature of 75°F.  Temperature and humidity will affect dry times.

MIX BY VOLUME (1:1)

Combine components by volume, mix thoroughly, and strain before spraying.

See Product Information Sheet #1014 for full usage details.

1	Part SkyBase® System 50™ Basecoat

1	Part TH07100™ Series Basecoat Reducer

#### POT LIFE

No pot life restrictions for uncatalyzed color.

Close container after use.  Occasional stirring may be desired to keep a uniform mix.

##### GUN SETUP

Fluid Tip	Air Pressure

HVLP Gravity:	1.3 - 1.5mm	6 – 10 PSI at the cap

HVLP Siphon:	1.3 - 1.5mm	6 – 10 PSI at the cap

Conventional Gravity:	1.3 - 1.5mm	45 - 55 PSI at the gun

Conventional Siphon:	1.3 - 1.6mm	45 - 55 PSI at the gun

## APPLICATION (As an overall or full-panel repair)

- Allow appropriate dry times of primers and sealers.

- Confirm color match is appropriate by testing color prior to application.

- Strain paint prior to application.

- Apply 2 – 3 wet coats, allowing 10 – 15 minutes flash between coats.

- Spray System 50™ Basecoat to complete hiding while making sure metallics are even prior to clearcoating.

- Allow final coat to flash for 20 – 30 minutes prior to applying clearcoat.

- When two-toning, apply first color and allow 40 – 60 minutes flash prior to taping for second color.  Make sure the first color is dry before taping to avoid tape tracking.

- See Product Information Sheet #1014 for full usage details.

BLENDING

- Use tack cloth to clean repair area.  Tack clothes may be used between coats of basecoat to eliminate overspray.                              Note:  Basecoat must be dry prior to re-tacking.

- Apply System 50 Basecoat until hiding.  Apply each coat beyond prior coat, keeping within the sanded blend area.  Allow proper flash between coats.  Lowering the air pressure on the last coat helps to blend out the color.  Do not dry spray color.

- Apply clearcoat beyond the basecoat and within the sanded blend area.

- For additional information on blending clearcoats, refer to the blending section found on the clearcoat product information sheets.

## PHYSICAL DATA

Dust Free:	10-15 minutes	Paint MSDS #22 (No Lead), #23 (Leaded)

Dry to Handle:	30 minutes (base must be cleared)	Reducer MSDS #1

RTS VOC:	6.40 lbs/gal (maximum)	P.I.S. #1014

Read and follow all technical product information, labels, and MSDS prior to application.  Keep product out of reach of children and animals.  Always wear proper safety equipment (respirator, gloves, eye, and clothing protection) when using this product.

# Text boxes

# System 50™ Sell Sheet

# Form #9015

BIG SKY

System 50™ SkyBase® Premium Basecoat color is designed to provide excellent coverage, fast dry times, and great metallic control.  This polyester and acrylic blended basecoat features easy repairability with no wrinkling.

Fast to Dry.  High Gloss.  Excellent Coverage.

## DESCRIPTION

## ADVANTAGES

- Excellent Coverage

- Fast Dry Times

- Great Metallic Control

- Easy Repairability

- No Wrinkling

###### Phone: (800) 328-4892 ● Fax: (330) 669-3965

###### 9287 Smucker Road ● Orrville, OH ● 44667

Website:  www.chemspec.co.za

www.montanabigsky.com

System 50™ SkyBase® Basecoat Color

BIG SKY

®

Rev. 6/15/04

SYSTEM 50™

SKYBASE® BASECOAT COLOR