CP6225 1K NON-SANDING PRIMER/SEALER 2.1 VOC

DESCRIPTION:

CP6225 1K NON-SANDING PRIMER/SEALER is a super smooth, one component primer Sealer. It can be used on all previously coated metal surfaces to provide a uniform surface prior to topcoat. CP6225 1K NON-SANDING PRIMER/SEALER has tremendous adhesion and excellent color holdout. Ready to spray; no mixing required. Pour unused sealer back in the can for future use.

FEATURES:

- Superior adhesion

- Excellent color hold-out

- Provides an extremely smooth surface

- Use “wet-on-wet”; no sanding required before topcoating

- Medium gray for ease of coverage

- Can be used on small bare steel cut-through spots

| COMPATIBLE SUBSTRATES: |
| --- |
|  | all previously coated metal surfaces to provide a uniform surface prior to topcoat Can be used on small bare steel cut-through spots |
| INSTRUCTIONS: |
|  | Shake or stir CP6225 1K NON-SANDING PRIMER/SEALER thoroughly before use. If using on a mixing machine, mix 2-3 minutes. Do not leave this primer on a mixing bank. |
| GUN SETUP: |
|  | Conventional Gravity 1.3mm -1.4mm 40-45 psi @ gun Siphon 1.3mm -1.4mm 40-45 psi @ gun HVLP gravity 1.3mm -1.4mm 8-10 psi @ gun |
| MIXING: |
|  | CP6225 1K NON-SANDING PRIMER/SEALER is ready to spray. No activator is required. |
| TINTING: |
|  | It is not recommended to tint CP6225 1K NON-SANDING PRIMER/SEALER. |
| SURFACE PREPARATION: |
|  | Wash area with soap and warm water. Thoroughly clean area with CP90 Wax and Grease Remover. CP905 Water Base Pre-clean can be used where stringent VOC restrictions are in effect. |
| APPLICATION: |
|  | Apply 1 uniform coat using a good quality spray gun with a 1.3mm-1.4mm fluid tip. Allow 15 minutes before topcoating. After overnight dry, clean, scuff and recoat before applying basecoat. |

TECHNICAL DATA

| Color: | Medium Gray |
| --- | --- |
| Activator/Hardener: | Not required |
| Reducers: California | Not required |
| Mix Ratio: | RTS (Ready To Spray) |
| Pot Life: | N/A |
| Number of Coats: | 1 |
| Flash Time before topcoating: | 15 minutes @75oF (23.9oC) |
| Recoat w/o sanding: | N/A |
| Dry to Sand: | N/A |
| Gun Set-Up Gravity Feed (HVLP) | 1.3mm - 1.4mm |
| Air Pressure @ Gun (HVLP) | 8 - 10 psi |
| Air Pressure @ Gun (Conventional) | 40 - 45 psi |
| V.O.C. Limit Regulatory Actual | 2.1 lbs/gal (252 g/l) 2.1 lbs/gal (252 g/l) .78 lbs/gal (93.6 g/l) |
| Sprayable V.O.C.* | 2.1 lbs/gal (g/l) |
|  | 2.1 lbs/gal (g/l) 4:1:1 mix with Zero V.O.C. Reducer |
| % Solids Sprayable by Weight | 31% |
| Coverage Sq. Ft. / gal @ 1 mil* | 481 sq. ft. |
| Package | Gallon |
| Per case (gallons) | 2 |
| Shelf Life | 12 months |