This acrylic enamel system is designed to offer a cost effective, fast drying, durable and easy-to-use single stage system for automotive refinishing.   When activated, System 10™ has good chemical resistance and gloss retention.

| Product Cross Reference Information Product comparisons are based on a similar product replacement. Performance and mix ratios may vary. |
| --- |
| DuPont | PPG | SW | BASF |
| Centari® | Delstar® | Acrylyd | Limco Select |

### DIRECTIONS FOR USE

Application recommendations are for an ambient shop temperature of 75°F.  Temperature and humidity will affect dry times.

MIX BY VOLUME (8:1:2)

Combine components by volume, mix thoroughly, and strain before spraying.

See Product Information Sheet #1031 for full usage details.

8	Parts System 10™ Color

1	Part MP1050™ Catalyst

2	Parts TH4000™ Series Reducer

#### POT LIFE

4 – 6 hours at 75°F

## ADDITIVES

Accelerator:  If needed, use 1 – 2 ounces of CR22ACC™ Accelerator per ready-to-spray gallon (or ¼ - ½ ounce per ready-to-spray quart).  Note:  System 10™ must be catalyzed in order for accelerator to be effective.

##### Fish Eye Eliminator:  If needed, add 1-2 ounces of CR22FEE™ per ready-to-spray gallon (or ¼ - ½ per ready-to-spray quart).

##### Note:  Use only Montana CR22FEE™ Fisheye Eliminator.  Other brands may be incompatible.

##### GUN SETUP

Fluid Tip	Air Pressure

HVLP Gravity:	1.3 – 1.6mm	6 – 10 PSI at the cap

HVLP Siphon:	1.3 – 1.8mm	6 – 10 PSI at the cap

Conventional Gravity:	1.3 – 1.6mm	45 – 55 PSI at the gun

Conventional Siphon:	1.3 – 1.8mm	45 – 55 PSI at the gun

## APPLICATION (As an overall or full-panel repair)

- Allow appropriate dry times of primers and sealers.

- Confirm color match is appropriate by testing color prior to application.

- Strain paint prior to application.

- Apply one medium wet coat and allow 15 – 20 minutes flash or until surface is hand slick.

- Apply a 2nd full wet coat.

- If a 3rd coat is needed, allow 20-minutes flash between 2nd and 3rd coats.  For best results, do not apply more than 3 coats.

- If metallics are being applied, apply one fog coat immediately after last coat, holding the spray gun back an additional 2 – 3”.  Raising the air pressure a few pounds will help even out metallics.

- See Product Information Sheet #1031 for full usage details.

## COMPOUNDING/POLISHING

- Air Dry:  24 – 36 hours at 75°F.

- See Product Information Sheet #1031 for full usage details.

## PHYSICAL DATA

Dust Free:	30-minutes	MSDS #14 (No Lead), #15 (Leaded)

Dry to Handle:	20-24 hours	Activator MSDS #6

VOC:	5.0 lbs/gal (maximum)	Reducer MSDS #1

P.I.S. #1031

Read and follow all technical product information, labels, and MSDS prior to application.  Keep product out of reach of children and animals.  Always wear proper safety equipment (respirator, gloves, eye, and clothing protection) when using this product.

# Text boxes

# System 10™ Sell Sheet

# Form #9018

®

This acrylic enamel system is designed to offer a cost effective, fast drying, durable and easy-to-use single stage system for automotive refinishing. When activated, System 10™ has good chemical resistance and gloss retention.

Fast Drying.  Durable.  Chemical Resistant.

## DESCRIPTION

## ADVANTAGES

- Cost Effective

- Fast Drying

- Durable and Easy to Use

- Excellent Chemical Resistance

###### Phone: (800) 328-4892 ● Fax: (330) 669-3965

###### 9287 Smucker Road ● Orrville, OH ● 44667

Website:  www.chemspec.co.za

www.montanabigsky.com

System 10™ Acrylic Enamel Single Stage Color

BIG SKY

Rev. 6/15/04

SYSTEM 10™

ACRYLIC ENAMEL COLOR SYSTEM

BIG SKY