System 20™ is an easy-to-use, quality designed, and economical coating that provides good gloss.  System 20™ has fast dry times and good coverage – an excellent choice when a quality economical finish is needed.

| Product Cross Reference Information Product comparisons are based on a similar product replacement. Performance and mix ratios may vary. |
| --- |
| DuPont | PPG | SW | BASF |
| Dulux® | Ditzco® | Kem Transport | Limco |

### DIRECTIONS FOR USE

Application recommendations are for an ambient shop temperature of 75°F.  Temperature and humidity will affect dry times.

MIX BY VOLUME (8:1:2)

Combine components by volume, mix thoroughly, and strain before spraying.

See Product Information Sheet #1032 for full usage details.

8	Parts System 20™ Color

1	Part MP2000™ Catalyst

2	Parts TH5000™ Series Reducer

#### POT LIFE

4 – 6 hours at 75°F

## ADDITIVES

Accelerator:  If needed, use 1 – 2 ounces of CR22ACC™ Accelerator per ready-to-spray gallon (or ¼ - ½ ounce per ready-to-spray quart).  Note:  System 20™ must be catalyzed in order for accelerator to be effective.

##### Fish Eye Eliminator:  If needed, add 1-2 ounces of CR22FEE™ per ready-to-spray gallon (or ¼ - ½ ounce per ready-to-spray quart).        Note:  Only use Montana CR22FEE™ Fisheye Eliminator.  Other brands may be incompatible.

##### GUN SETUP

Fluid Tip	Air Pressure

HVLP Gravity:	1.3 – 1.6mm	6 – 10 PSI at the cap

HVLP Siphon:	1.3 – 1.8mm	6 – 10 PSI at the cap

Conventional Gravity:	1.3 – 1.6mm	45 – 55 PSI at the gun

Conventional Siphon:	1.3 – 1.8mm	45 – 55 PSI at the gun

## APPLICATION (As an overall or full-panel repair)

- Allow appropriate dry times of primers and sealers.

- Confirm color match is appropriate by testing color prior to application.

- Strain paint prior to application.

- Apply one medium wet coat and allow 15 – 20 minutes flash or until surface is hand slick.

- Apply a 2nd full wet coat.

- If a 3rd coat is needed, allow 20-minutes flash between 2nd and 3rd coats.  For best results, do not apply more than 3 coats.

- If metallics are being applied, apply one fog coat immediately after last coat, holding the spray gun back an additional  2 – 3”.  Raising the air pressure a few pounds will help even out metallics.

- See Product Information Sheet #1032 for full usage details.

## COMPOUNDING/POLISHING

- Air Dry:  24 – 36 hours at 75°F.

- See Product Information Sheet #1032 for full usage details.

## PHYSICAL DATA

Dust Free:	30-minutes	MSDS #12 (No Lead), #13 (Leaded)

Dry to Handle:	Overnight	Activator MSDS #6

VOC:	5.0 lbs/gal (maximum)	Reducer MSDS #1

P.I.S. #1032

Read and follow all technical product information, labels, and MSDS prior to application.  Keep product out of reach of children and animals.  Always wear proper safety equipment (respirator, gloves, eye, and clothing protection) when using this product.

# Text boxes

# System 20™ Sell Sheet

# Form #9020

®

System 20™ is an easy-to-use, quality designed, and economical coating that provides good gloss.  System 20™ has fast dry times and good coverage – an excellent choice when a quality economical finish is needed.

Fast Dry Times.  Economical.  Good Gloss.

## DESCRIPTION

## ADVANTAGES

- Easy-To-Use

- Economical

- Good Gloss

- Excellent Coverage

- Provides a Quality Finish

###### Phone: (800) 328-4892 ● Fax: (330) 669-3965

###### 9287 Smucker Road ● Orrville, OH ● 44667

Website:  www.chemspec.co.za

www.montanabigsky.com

System 20™ Synthetic Enamel Color System

BIG SKY

Rev. 6/16/05

SYSTEM 20™

SYNTHETIC ENAMEL COLOR SYSTEM

BIG SKY