Our 3.5 VOC Compliant high-solids, single stage polyurethane is the ultimate choice for durability and excellent chemical resistance.   With a deep finish, System 35™ provides excellent flow, leveling and flexibility, good color holdout, and is both impact and UV resistant – it even stands up to Skydrol.

| Product Cross Reference Information Product comparisons are based on a similar product replacement. Performance and mix ratios may vary. |
| --- |
| DuPont | PPG | SW | BASF |
| Imron® 5000™ 3.5 | Delta® DGHS 3.5 | Sunfire 3.5 | Diamont 3.5 |

### DIRECTIONS FOR USE

Application recommendations are for an ambient shop temperature

of 75°F.  Temperature and humidity will affect dry times.

MIX BY VOLUME (3:1)

Combine components by volume, mix thoroughly, and strain before spraying.

See Product Information Sheet #1017 for full usage details.

3	Parts System 35™ Color

1	Part PO35A™ Activator (normal or slow)

Optional ½ part reduction with TH028™ or TH035™ Low VOC Reducer

#### POT LIFE

1 –2 hours at 75°F

Note:  We suggest mixing only enough product for a single coat.

## ADDITIVES

Accelerator:  If needed, use 1 – 2 ounces of PE35ACC™ Accelerator per ready-to-spray gallon (or ¼ - ½ ounce per ready-to-spray quart).  Note:  the use of PE35ACC™ will extend pot life and increase cure rate by approximately 4-hours.

##### Fish Eye Eliminator:  If needed, add 1-2 ounces of CR22FEE™ per ready-to-spray gallon (or ¼ - ½ ounce per ready-to-spray quart).        Note:  Use only Montana CR22FEE™ Fisheye Eliminator.  Other brands may be incompatible.

##### GUN SETUP

Fluid Tip	Air Pressure

HVLP Gravity:	1.3 – 1.5mm	6 – 10 PSI at the cap

HVLP Siphon:	1.3 – 1.6mm	6 – 10 PSI at the cap

Conventional Gravity:	1.3 – 1.5mm	45 – 55 PSI at the gun

Conventional Siphon:	1.3 – 1.6mm	45 – 55 PSI at the gun

## APPLICATION (As an overall or full-panel repair)

- Allow appropriate dry times of primers and sealers.

- Confirm color match is appropriate by testing color prior to application.

- Strain paint prior to application.

- Apply one medium wet coat and allow 20-minutes flash.

- Apply a 2nd full wet coat.

- If a 3rd coat is needed, for color hiding, allow 20-minutes flash between 2nd and 3rd coats, and apply a light coat.  For best results, do not apply more than 3 coats.

- If metallics are being applied, apply one fog coat immediately after last coat, holding the spray gun back an additional 2 – 3”.  Raising the air pressure a few pounds will help even out metallics.

- See Product Information Sheet #1017 for full usage details.

## COMPOUNDING

- Air Dry:  24 – 72 hours at 75°F.

- See Product Information Sheet #1017 for full usage details.

## PHYSICAL DATA

Dust Free:	60-90 minutes	MSDS #20 (No Lead), #21 (Leaded)

Dry to Handle:	Overnight	Activator MSDS #6

VOC:	3.5 lbs/gal (maximum)	Reducer MSDS #1

P.I.S. #1017

Read and follow all technical product information, labels, and MSDS prior to application.  Keep product out of reach of children and animals.  Always wear proper safety equipment (respirator, gloves, eye, and clothing protection) when using this product.

# Text boxes

# System 35™ Sell Sheet

# Form #9016

BIG SKY

Our 3.5 VOC Compliant high-solids, single stage polyurethane is the ultimate choice for durability and excellent chemical resistance.   With a deep finish, System 35™ provides excellent flow, leveling and flexibility, good color holdout, and is both impact and UV resistant – it even stands up to Skydrol.

High Solids.  VOC Compliant.  UV Resistant.

## DESCRIPTION

## ADVANTAGES

- Low 3.5 VOC Meets Strictest Regulations

- High Solids

- Excellent Chemical Resistance

- Provides a Deep Finish

BIG SKY

System 35™ Polyurethane Single Stage Color

###### Phone: (800) 328-4892 ● Fax: (330) 669-3965

###### 9287 Smucker Road ● Orrville, OH ● 44667

Website:  www.chemspec.co.za

www.montanabigsky.com

®

SYSTEM 35™

3.5 VOC POLYURETHANE COLOR SYSTEM

Rev. 6/16/05